CAMSERFİX

Cement Based Glass Brick Laying Mortar & Joint Filler

Cement Based Glass Brick Laying Mortar & Joint Filler

DEFINITION

Cement Based Glass Brick Laying Mortar & Joint Filler

CHARACTERISTICS

- It has both adhesive and joint filling function.

- It is comfortable and easy to apply.

- It can be used for both interior and exterior surfaces.

APPLICATION FIELDS

Used for glass brick laying and filling the joints in all fields.

STORAGE & PACKING

- 20 kg kraft bags, in the sling or shrink covered pallets upon request.

- 1 year from the date of manufacture if stored in unopened original package; under dry, frost free conditions and arranged maximum 8 bags one above the other. Suggested to be consumed in 1 week after the package is opened.

SPECIAL SUGGESTIONS

- The surface must be purified from form oil, dust, paint and adherence reducing materials.

- No other materials (lime, cement, gypsum etc..) should be added to the prepared mortar.

- Suggested that the application is done between +5°C, +35°C.

- Don’t go beyond the application field and rules.

- As it is cement based product, do not smell it directly. Wash your eyes in case of contact. Call your doctor if it is necessary.

# For detailed information please request security data sheet.

# Contact  us for the other application fields and for your technical questions.

APPLICATION RULES

For using as laying mortar,

- CAMSERFİX; is mixed by hand or preferably with an electrical drill (7 lt. water / 20 kg bag).

- To prepare the mortar :

- Add some water to a plastic pot, and than add CAMSERFİX and mix.

- Wait for 5 minutes and mix again to obtain a homogeneous product.

- Ready mortar is applied to both glass bricks, application thickness should be 3-10 mm.

- After the application of brick laying, joint application should start at least in 24 hours.

For using as joint filler,

- CAMSERFİX; is mixed by hand or preferably with an electrical drill (7,6 lt water / 20 kg bag).

- To prepare the mortar:

- Add some water to a plastic pot, and than add CAMSERFİX and mix.

- Wait for 5 minutes and mix again to obtain a homogeneous product.

- Ready mortar is applied in the  appropriate thickness with a rubber spatula.

- Approximately 45 minutes after the application, the surface is cleaned with a damp sponge.

- Do not use the mortar that are out of date.

CURE

For high performance the application field should be dampened after 1 day.

CONSUMPTION

Approximately 2 kg / m² for 8 mm joint thickness.

TECHNICAL DATA

| ### water/ powder ratio (laying mortar), % | 35 |
| --- | --- |
| ### water / powder ratio (joint filler), % | 28 |
| # Dry bulk density ,kg/m³ | 1000 ± 100 |
| Wet bulk density, kg/m³ | 1700 ± 200 |
| Comprehensive Strength, N/mm² | > 11 |
| Flexural strength, N/mm² | > 3,5 |