DOLFİN

Thin Levelling Mortar for Concrete Surfaces

# Thin Levelling Mortar with high adhesion

### DEFINITION

# Thin Levelling Mortar for Concrete Surfaces

### CHARACTERISTICS

- High resistance to water.

- No need for priming.

# APPLICATION FIELDS

Used for levelling and plastering the interior and exterior faces of the fair-faced concrete surfaces and for repairing the wall plasters.

STORAGE & PACKING

- 25 kg kraft bags, in the sling or shrink covered pallets upon request.

- 1 year from the date of manufacture if stored in unopened original package; under dry, frost free conditions and arranged maximum 8 bags one above the other. Suggested to be consumed in 1 week after the package is opened.

SPECIAL SUGGESTIONS

- In every case, the surface must be cleaned from dust, oil and paint.

- Application field must be dampened with water.

- No other materials (lime, cement, gypsum etc..) should be added to the prepared mortar.

- Suggested that the application is done between +5°C, +35°C.

- Don’t go beyond the application field and rules.

- As it is cement based product, do not smell it directly. Wash your eyes in case of contact. Call your doctor if it is necessary.

# For detailed information please request security data sheet.

# Contact  us for the other application fields and for your technical questions.

## APPLICATION RULES

- DOLFİN is mixed with an electrical drill or by hand ( 4-5 lt. water/ 25 kg bag).

- To prepare the mortar

- Water is poured into a plastic container, then DOLFİN is added and mixed.

- Should be waited for 5 minutes and mixed again to obtain a fully homogenous product.

For levelling ;

- If necessary the holes must be filled by a trowel.

- DOLFİN is applied by a steel trowel 3- 5 mm in one coat , max.10 mm in  total. It must be equal on the surface.

- If it is applied more then one coat, must be waited for 5-6 hours between the coats and the first coat must be dampened. Total plaster thickness must not be more than 7 mm.

- For the final coat application on DOLFİN, according to the weather conditions, must be waited for at least 7 days.

For repairing :

1. The surface must be cleaned from plaster pieces and must be roughed.

2. Surfaces’ edge which is made by breaking must be cut vertical.

3. If there is a water flow on the surface it must be drained.

4. The repairing surface must be covered with DOLFİN. First coat is applied in 5 mm thickness and waited for 5-6 hours, when the mortar is absorbed it is applied in 5 mm thickness once more. The total thickness must be max. 10 mm.

# CURE

For the durability of plaster, in 7 days after the application, depending on weather conditions the surface must be dampened at intervals.

### CONSUMPTION

1,5 kg / m²/mm

#### TECHNICAL DATA

| # Dry bulk density, kg/m³ | 1250 ± 150 |
| --- | --- |
| Wet bulk density, kg/m3 | 1750 ± 200 |
| ### Compressive Strength, N/mm² | > 5 |
| Flexural Strength, N/mm² | > 1,5 |
| Adhesion, N/ mm² | > 0,3 |