AKFİN®

Cement Based Satin Putty

##### APPLICATION FIELD

Used for obtaining a smooth final coat surface on concrete surfaces and polished cement-plastered surfaces on the interior and exterior faces of the buildings.

White and grey colour options are available

##### PROPERTIES

Provides a smooth finish on the top coat.

# Polymer additive.

It is used for indoor and outdoor surfaces.

Water and frost resistant.

White and grey colour are available.

##### APPLICATION

SURFACE PREPARATION

The surface of application will always be free of materials such as form oil, dust, paint, etc.

Moving parts with low adherence should be moved away from the surface. Precautions against dusting should be taken on plastered surfaces. Application is started after dampening the surface.

##### PREPARATION AND APPLICATION OF THE MORTAR

##### A proper amount of water will be put inside the mixing vessel (8,5 - 9,5 litre of water for 25 kg bag).

##### Powder material will be added and mixed with hand mixer at low speed.

##### After resting for 5 minutes, the plaster will be mixed until achieving a homogeneous mixture.

##### The mortar prepared should be applied with a steel trowel.

##### It should be applied as two coats for thicker applications and the second coat should be applied when the first coat is set adequately.

##### CONSUMPTION

For 1 mm thickness: 1,2 kg/m²

##### TECHNICAL DATA

|  | Dry Film Thickness |  |  |  |  |  |  | > 400; E5 |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Particle Size, mm |  |  |  |  |  |  | <300; S2 |  |  |
|  | Water Vapour Transmission Rate, g/(m².day) |  |  |  |  |  |  | V0 |  |  |
|  | Water Transmission Rate, kg/(m².hour0,5) |  |  |  |  |  |  | W0 |  |  |
|  | Crack Bridging |  |  |  |  |  |  | A0 |  |  |
|  | CO2 Permeability |  |  |  |  |  |  | C0 |  |  |
|  | Resistance to Mould Growth |  |  |  |  |  |  | K2 |  |  |
| TS EN 1062-1 |  | G3 | E5 | S2 | V0 | W0 | A0 |  | C0 | K2 |

##### PACKAGING AND STORAGE

- Available in 25 kg polyethylene-reinforced paper bags, delivered in pallets or as sling-bags upon request.

- It is recommended to be consumed in 1 year from the date of production if stored in its original package without opening the package under dry, frost free conditions and is stacked as maximum 8 bags. It should be consumed in 1 week after opening the bag. The bag should be tightly closed when it is not used.

##### RECOMMENDATIONS

##### No other materials (lime, cement, gypsum, etc.) should be added to the prepared mortar.

##### Plaster should not be used again by mixing with water or dry plaster if its application time has expired.

##### Not suitable for applying on sheathing.

##### AKFIN® will be applied at least 7 days later than the application of the plaster.

##### The application is performed between +5°C and +35°C.

##### AKFIN® will be protected against quick drying under windy weather conditions.

##### It should not be applied on frozen surfaces.

##### Do not apply under direct sunlight.

##### Do not go beyond the application field and the rules.

##### Do not inhale it directly. Wash your eyes with plenty of water in case of contact with eyes, seek medical attention if required.

##### For detailed information, please request the safety data sheet.

##### Contact us for your technical questions and for your questions about all other application

##### CERTIFICATE OF CONFORMITY

|  | TS 7847/ June 2012 / E5-S2-K2 |
| --- | --- |

Above stated data obtained in lab conditions. Entegre will not be liable for any defect in product occurring by reason of events or conditions not within its control such as misuse, mishandling, improper storage or improper installation.

Entegre reserves the right to revise the information contained herein without prior notice.

ENTEGRE HARÇ SAN. Ve TİC. A.Ş

HÜSEYİNLİ VILLAGE, BEYKOZ STREET. No:222/4 34799 Çekmeköy/İSTANBUL T: 0216 434 50 96 F: 0216 434 50 31 www.entegreharc.com.tr