FiNEL® iÇ

Cement-Based Final Coat Plaster - Interior

FIELD OF APPLICATION

##### Used for obtaining a final coat surface on concrete surfaces and polished surfaces on the interior faces of the buildings.

##### PROPERTIES

Allows breathing of the surfaces.

Provides a smooth surface on the final coat.

It has a white colour.

It has polymer additives

##### APPLICATION

SURFACE PREPARATION

##### The surface of application willl always be free of materials such as form oil, dust, paint, etc.

##### Moving parts with low adherence should be moved away from the surface.

##### Application is initiated after dampening the surface. Precautions against dusting should be taken on plastered surfaces.

##### PREPARATION AND APPLICATION OF THE MORTAR

A proper amount of water will be put inside the mixing container (9-9,5 l water/25 kg bag).

Powder material will be added and mixed with hand mixer.

After resting for 5 minutes, the plaster should be mixed until achieving a homogeneous mixture.

The mortar prepared should be applied with a steel trowel.

Application thickness should be 2-3 mm.

It should be applied as two coats for thicker applications and the second coat should be applied when the first coat is set adequately.

##### CONSUMPTION

1.2 kg/m² for 1 mm of thickness

##### TECHNICAL DATA

| Dry Bulk Density of Hardened Mortar, kg/m³ | 1200 ± 200 |
| --- | --- |
| Compressive Strength, N/mm² | > 2 (CS I) |
| Adhesion Strength, N/mm² | ≥ 0.15 (FP:B) |
| Capillary Water Absorption, kg/m².min0.5 | W0 |
| Water Vapour Permeability Coefficient (µ) | ≤ 25 |
| Average Thermal Conductivity (W/m.K) | ≤ 0.49 |
| Reaction to Fire | A1 |

##### PACKAGING AND STORAGE

- Available in 25 kg paper bags, delivered in pallets or as sling-bags upon request.

- It is recommended to be consumed in 1 year from the date of production if stored in its original package without opening the package under dry, frost free conditions and is stacked as maximum 8 bags, and in 1 week after opening the package. Package should be tightly closed when it is not used.

##### RECOMMENDATIONS

- No other materials (lime, cement, gypsum, etc.) should be added to the prepared mortar.

- Plaster should not be used again by mixing with water or dry plaster if its application time has expired.

- FINEL® IÇ will be applied at least 7 days later than the application of the plaster.

- It is recommended the application to be performed between +5°C and +35°C.

- FINEL® IÇ will be protected against quick drying under windy weather conditions.

- It should not be applied on frozen surfaces.

- Do not apply under direct sunlight.

- Do not go beyond the application field and the rules.

- Do not inhale it directly. Wash your eyes with plenty of water in case of contact with eyes, seek medical attention if required.

- For detailed information, please request the safety data sheet.

- Contact us for your technical questions and for your questions about all other application conditions.

##### CERTIFICATE OF CONFORMITY

|  | TS EN 998-1 / February 2017 / A1-GP-CSI |
| --- | --- |

Above stated data obtained in lab conditions. Entegre will not be liable for any defect in product occurring by reason of events or conditions not within its control such as misuse, mishandling, improper storage or improper installation.

Entegre reserves the right to revise the information contained herein without prior notice.

ENTEGRE HARÇ SAN. Ve TİC. A.Ş

HÜSEYİNLİ VILLAGE, BEYKOZ STREET. No:222/4 34799 Çekmeköy/İSTANBUL T: 0216 434 50 96 F: 0216 434 50 31 www.entegreharc.com.tr