PRIMEL PLUS®

Cement-Based Ready-Mixed Primer

FIELD OF APPLICATION

##### Primer used for increasing adherence on the surface before application of plasters on aerated concrete, pumice concrete bright fair faced surfaces, concrete ceilings and walls.

##### PROPERTIES

Polymer modified.

Provides a firm ground during the preparation of the surface before plastering.

Provides good adhesion with the lower surface and serves as a bond between the plaster to be applied on it and the lower surface.

Provides a controlled water absorption transfer between surfaces with high and low water absorption rates.

It may be easily and rapidly applied.

##### APPLICATION

SURFACE PREPARATION

##### The surface shall always be free of form oil, dust, paint and materials that reduce adherence.

##### Repair of the cracks and holes shall be made using appropriate Entegre Repair Mortars before application.

##### Application surface shall be dampened with water, if required.

##### PREPARATION AND APPLICATION OF THE MORTAR

##### PRIMEL PLUS® shall be mixed with power mixer or by hand (13-14 l water/50 kg bag).

##### After resting for 5 minutes, it shall be mixed until achieving a homogeneous mixture.

##### PRIMEL PLUS® shall be applied with trowel or trolien.

##### Final surface shall have a thickness of 4-7 mm and a textured surface appearance.

##### CONSUMPTION

Approximately 3.5-4 kg/m² with trowel, and approximately 2.5-3 kg/m² for trolien.

##### TECHNICAL DATA

| Dry Bulk Density of Hardened Mortar, kg/m³ | 1900 ± 200 |
| --- | --- |
| Compressive Strength, N/mm² | ≥ 6.0 (CS IV) |
| Adhesion Strength, N/mm² | ≥ 0.3 (FP:A) |
| Capillary Water Absorption, kg/m².min0.5 | W0 |
| Water Vapour Permeability Coefficient (µ) | ≤ 25 |
| Average Thermal Conductivity, W/m.K | ≤1.28 |
| Reaction To Fire | A1 |

##### PACKAGING AND STORAGE

##### Available in 50 kg paper bags, delivered in pallets or as sling-bags upon request.

##### It is recommended that the product shall be  consumed in 1 year from the date of production if stored in its original package without opening the package under dry, frost free conditions and is stacked as maximum 8 bags, and in 1 week after opening the package

##### RECOMMENDATIONS

##### No other materials (lime, cement, gypsum, etc.) shall be added to the prepared mortar.

##### Always consult the technical department about the plaster to be applied on it before using it as the type and application conditions of the plaster to be applied on the surface after application of the primer shall affect the surface adherence.

##### It is recommended the application shall be performed between +5°C and +35°C.

##### PRIMEL PLUS® shall be protected against quick drying under windy weather conditions.

##### You shall wait at least 1 days for the application to be performed on the PRIMEL PLUS® depending on the ambient temperature.

##### Surface shall be watered in specific intervals within 1 days after the application to ensure its strength.

##### Do not go beyond the application field and the rules.

##### Do not inhale it directly. Wash your eyes with plenty of water in case of contact with eyes, seek medical attention if required.

##### For detailed information, please request the safety data sheet.

##### Contact us for your technical questions and for your questions about all other application conditions.

##### CERTIFICATE OF CONFORMITY

|  | TS EN 998-1 / July 2011 Complies with A1-GP-CS IV-W0 Class |
| --- | --- |

Above stated data obtained in lab conditions. Entegre will not be liable for any defect in product occurring by reason of events or conditions not within its control such as misuse, mishandling, improper storage or improper installation.

Entegre reserves the right to revise the information contained herein without prior notice.

ENTEGRE HARÇ SAN. Ve TİC. A.Ş

HÜSEYİNLİ VILLAGE, BEYKOZ STREET. No:222/4 34799 Çekmeköy/İSTANBUL T: 0216 434 50 96 F: 0216 434 50 31 www.entegreharc.com.tr