SATENPER®

Satin Plaster

(Makes surface ready for painting)

##### APPLICATION FIELD

It is used as a topcoat on gypsum or cement based plasters in interior surfaces and on surfaces coated with fine plaster.

##### PROPERTIES

Provides comfortable and easy application with long working life and paste consistency.

Gives excellent results before painting.

##### APPLICATION

SURFACE PREPARATION

Surface to be treated; mould oil, dust, paint, such as materials must be cleaned.

MORTAR PREPARATION AND APPLICATION

First add water to the mixing bowl, then add the SATENPER® (15,5-16,5 L water/30 kg bag) and mix until the lumps go away. Wait 5 minutes, and mix again to obtain a homogeneous mixture.

Prepared mortar is applied to the surface by a steel trowel with a thickness of 1-2 mm.

Before painting, the surface is finished with a fine sandpaper.

##### CONSUMPTION

About 1,0 kg/m²  for 1 mm thickness

##### TECHNICAL DATA

| Compressive Strength, N/mm² | ≥ 2,0 |
| --- | --- |
| Bond Strength, N/mm² | ≥ 1,0 |
| Initial Setting Time, min | > 20 |
| Reaction to Fire | A1 |

##### PACKAGING AND STORAGE

- In 30 kg PP bags, it is shipped with pallets if requested.

- In dry and frost free environment, in its original package unopened, it must be consumed within 6 months from the date of production, provided that it is stocked as 8 rows. It is recommended to consume within 1 week after opening the bag.

##### RECOMMENDATIONS

- No foreign material (lime, cement, gypsum etc.) must be added to the prepared mortar.

- It is recommended to apply at temperature between +5 °C, +35 °C.

- At least 3 days must be waited for applications on SATENPER® depending on the ambient temperature.

- Do not use out of the application field and instructions.

- Do not smell directly. In case of contact with eyes, rinse immediately with plenty of water and seek.

- Please request the product safety data sheet for more information.

- Please contact us for your technical questions regarding all other application conditions.

##### CERTIFICATE OF CONFORMITY

TS EN 13279-1 / February 2009 / C6-20-2,0

Public Work Items No: 04,458/E

Above stated data obtained in lab conditions. Entegre will not be liable for any defect in product occurring by reason of events or conditions not within its control such as misuse, mishandling, improper storage or improper installation.

Entegre reserves the right to revise the information contained herein without prior notice.

ENTEGRE HARÇ SAN. Ve TİC. A.Ş

HÜSEYİNLİ VILLAGE, BEYKOZ STREET. No:222/4 34799 Çekmeköy/İSTANBUL T: 0216 434 50 96 F: 0216 434 50 31 www.entegreharc.com.tr